## Slide 1: Introduction to Solid Breeders
MAE 237D Winter 2016
UCLA
JTVL

## Slide 2: Solid Breeder Material Technology

## Slide 3: Why are we interested in solid breeder concepts?
Safety advantages of solid breeders
  Low tritium mobility
  Low stored chemical energy
Solid breeder materials narrowed down to ternary oxides of lithium
  Li2TiO3, Li4SiO4, Li2ZrO3
Oxides have desirable characteristics
  High lithium densities
  High melting temperatures
  Good tritium release
  Good thermophysical/thermochemical
  Desirable neutronics

## Slide 4: Material Requirements
Neutronics
Thermochemical Properties
Tritium Release
Physical/Thermo-physical Properties
Compatibility
Radiation Effects
Fabrication

## Slide 5: Neutronics
Functional requirement of tritium breeding is among the most critical
  Oxide material can not interfere with the ability to capture neutrons
Neutron multiplication a necessity for all but lithium oxide

## Slide 6: Thermochemical Properties: Solubility Calculations
Solubility of tritium in ceramic material is a major concern
(Simplified) thermochemical model to estimate solubilities
Very high solubility
Good solubility characteristics

## Slide 7: Stoichiometry after Li-burnup
Lithium in ceramics is slowly transmuted into tritium
Stoichiometry and kinematics of ceramics in lithium-depleted materials has great uncertainty
  e.g. LiAl5O8 is more stable than Al2O3
  Free energy changes and Kp values overestimated
Eutectic temperatures often much lower than melt temperatures
  e.g. Li4SiO4 ceramics develop an excess of silica, max temperature 1300 C drops to 1024 C

## Slide 8: Tritium Release
Mechanistic steps of tritium release
  Bulk diffusion
  Grain boundary migration
  Desorption of tritium (T2O)
  Percolation of tritium through pores internal to the solid ceramic toward purge gas
  Convective mass transfer out of blanket via purge channels
Diffusion of sphere, radius rp:
High uncertainty
Residency time measured in experiments
Inventory related to measured residency time

## Slide 9: Minimum Temperature for Solid Breeders
Residence times measured to be temperature dependent (consistent with diffusion-controlled processes)
Define minimum temperature such that inventory will not exceed 1kg/GW
Chart: Minimum Temperatures
| Li2O | LiAlO2 | Li2SiO3 | Li2Si | LiAl | Li7Pb2 | Li2TiO3 | Li2ZrO3 | Li4SiO4
STARFIRE, 1981 | 410 | 500 | 420 | 480 | 300 | 320
Clemmer, 1980 | 410 | 500 | 420 | 480 | 300 | 320 | 420 | 420
Johnson et al., 1988 | 400 | 450 | 410 | 400 | 350

## Slide 10: Maximum Temperature for Solid Breeders
Inventory related to square of diffusion length
Maintain ceramic grain size as small as possible
Grain growth during sintering & irradiation induced sintering
Keep in mind the stoichiometric changes due to lithium burn-up
Chart: Maximum Temperatures
| Li2O | LiAlO2 | Li2SiO3 | Li2Si | LiAl | Li7Pb2 | Li2TiO3 | Li2ZrO3 | Li4SiO4
STARFIRE, 1981 | 910 | 850 | 610 | 420 | 380 | 390
Clemmer, 1980 | 910 | 850 | 610 | 350 | 310 | 330 | 820 | 860
Johnson et al., 1988 | 800 | 832 | 800 | 981 | 666
Johnson & Clemmer, 1981 | 750 | 855 | 820 | 860 | 670

## Slide 11: Physical/Thermo-physical Properties
Thermal conductivity a major factor – removing large nuclear heat loads
Elastic moduli a reflection of atomic bond strength
  Qualitative information on lattice defects
  Irradiation of LiAlO2 (1020 n/cm2)
    400 C, no change
    600 C, 10% reduction
Compressive strength not sensitive up to 2% at.% burn-up of lithium

## Slide 12: Compatibility
Main concern is corrosion and tritium entrapment
Ternary oxides (Li2TiO3, Li4SiO4, etc.) relatively unreactive to structural materials
LiO, in the presence of any moisture, highly corrosive
Compatibility with neutron multiplier
  BeO layer slows the diffusion of T out of Be, increasing inventory
  Beryllides (e.g. Be12Ti) allow possibility of mixed volumes of breeder & multiplier

## Slide 13: Radiation Effects – Radiation Damage
Neutron capture of 6Li results in…
  2 large gas atom production
  Lithium vacancy
Several anticipated radiation damage mechanisms:
  Displacement damage
  Vacancies
  Loops, clusters, etc.
  Interstitials
Heat transfer in ceramics depends on phonon transport along lattices
  Phonon scattering at defect sites will disrupt heat transfer
  Though up to ITER-relevant fluence (~1024 n/m2), no significant reduction has been seen in some ceramics

## Slide 14: Danger of Daughter Nuclides
Selling point of fusion is environmentally benign impact
Choice of ceramic material must not abandon this ideal
  Long-lived daughter nuclides should be avoided
  Materials should meet requirements for near-surface burial as radioactive waste
Li2TiO3 and Li4SiO4 are most attractive from this perspective

## Slide 15: Fabrication
Example of wet-slurry droplet technique from NFRI
Mixing
Shaping
Sintering
Li2TiO3 Powder
PVA Solution
Mixing
Dropping into Glycerin
including Boric Acid
Drying
Sintering
Fabrication Process
PVA Solution
Li2TiO3 Powder
Any feasible technique must be able to scale to industrial production

## Slide 16: Neutron Multiplication in Solid Breeders
Two beryllium reactions have the possibility to produce tritium
Tmelt = 1250 C
  Exist as solid form
Corrosion concerns
Beryllium poisoning
Tritium inventory

## Slide 17: Novel neutron multiplication options
More advantages of Be12Ti
  More compatible with steel than Be
  Less swelling than Be
  T inventory is significantly lower than Be
  High Be density maintains n multiplication
  Option for mixing with ceramic material

## Slide 18: Introduction to Solid Breeder Analysis
Solid Breeder Thermal Management and Temperature Window
Purge Gas & Coolant
Phenomenological Models of Packed Beds
Continuum Modeling of Packed Beds
Discrete Element Modeling of Packed Beds

## Slide 19: Example Japanese solid breeder
Coolant flow
Purge gas

## Slide 20: Why we need such precision on thermal management?
Breeding blankets experience high volumetric heating from fusion neutrons (and secondary γ-rays)
Long heat path from generation to coolant in SB
  Heat conducted through bed (poorly) toward container
  HT through interface with container (dependent on good contact)
  Purge gas will not help as coolant
Coupling between mechanical and thermal loads due to contact conductance of granular media

## Slide 21: Why we need such precision on thermal management?
Large thermal and mechanical stresses on beds…
  Cracking/crushing of individual pebbles
  Inter-particle creep/necking
  Sintering in hot spots
Tritium inventory & diffusion concerns dictate a narrow operational temperature window
Models must precisely predict thermomechanical interactions to allow tritium release with higher power density

## Slide 22: Purge Gas – Tritium extraction
NOT meant to act as coolant
  Any heat picked up by purge gas must be removed before entering cryogenic sieve, etc. for tritium extraction
Pressure drop across packed bed
  Low Reynolds flow
  Kozeny-Carman correlation most appropriate
Tritium permeation from purge gas into structure and into coolant is a safety concern

## Slide 23: Coolant
Requirements
  Must maintain containment below structural limits (~650 C for steel)
  Must move high quality heat into power extraction cycle
High pressure helium or water (reactivity with LiO a concern)
Uniform flow partitioning is a design challenge

## Slide 24: Phenomenological Models of Heat Transfer
Heat transfer through two phases of solid and fluid
First historical treatment began with limiting cases
  Maximum heat transfer in parallel
  Minimum in series
Solid
Fluid
Solid
Fluid
Parallel
Series
TH
TL

## Slide 25: Effective conductivity models
Zehner and Schlunder introduced a model in 1970 considering a unit cell and empirically fit to data
  Modified later with Bauer to include radiation effects
  Become de-facto correlation for first order calculation in packed beds
  Uncompressed pebble beds

## Slide 26: Direct measurements of keff with transient hot wire technique
Reliable technique for measuring effective conductivity of granular materials
Pulse of current
Thermocouples
Chris’s setup at UCLA

## Slide 27: Effective conductivity weakly a function of strain
Indicative of granular conductivity a function of contact pressures
Li4SiO4
Li2TiO3

## Slide 28: Effective thermal expansion
Li2TiO3
Roughly 80% of the bulk value

## Slide 29: Transient Discrete Element Method
Spring/dashpot coefficients are from Hertz theory for contacting elastic spheres
based solely on material and geometric properties
A Velocity-Verlet integration algorithm
Heat transfer model captures conduction between particles through contact
J
I
Q

## Slide 30: How does configuration effect temperature distribution when pebbles break?
configuration
configuration
20 mm
~50 mm
~50 mm
20 mm

## Slide 31: Multi-scale governing equations
Pebbles (DEM)
Helium (volume-averaged CFD)
Exchange coefficients
More details of numerical method:
Van Lew, J. T., Ying, A., & Abdou, M.
http://doi.org/10.13182/FST14-937
DEM material implementation models:
Van Lew, J. T., Park, Y.-H., Ying, A., & Abdou, M.
http://doi.org/10.1016/j.fusengdes.2015.06.012

## Slide 32: Granular fragmentation modeling
Several approaches used in studies at KIT for broken pebble modeling
  Reduced Young’s modulus
  Reduced radius
Previous approach from UCLA had the broken pebbles `deleted’
New approach considers fragmentation and resettling
Uncoupled fragmentation impact from fragmentation predictions
,
,

## Slide 33: Example of flow field through beds
Helium purge gas ‘regulates’ the temperature of fragments to equilibrate with nearby pebbles

## Slide 34: Pebble bed cross-sections
Identify several zones for discussion
configuration
configuration

## Slide 35: Reduced Mean Temperature Profiles
Solid line = configuration
Dashed line = configuration
Calculated for n pebbles in volume of slice thickness
Asymmetric lump in
High peak in

## Slide 36: Maximum Temperature Rise
Many loose fragments in cause ~25% jump in T
Only 10% increase in maximum T

## Slide 37: Local packing fraction changes due to fragment settling

## Slide 38: Example of travel of fragments for case with 5% crushed pebbles
m
m
initial
final

## Slide 39: Vertical travel of fragments for case with 5% crushed pebbles
~8% of fragments travel more than 2 mm
~60% of fragments travel less than 1 mm