## Slide 1: Required readings
M.A. Abdou, L.J. Wittenberg, and C.W. Maynard, A Fusion Design Study of Nonmobile Blankets with Low Lithium and Tritium Inventories, Nuclear Technology, 26: 400–419 (1975).
http://www.fusion.ucla.edu/abdou/Presentation%20Web%20Page.html
  Search for “Lectures in IPR, India”
  Lecture 2: Solid Breeder Blanket Concepts

## Slide 2: Lithium cross sections

## Slide 3: Neutron multiplier cross sections

## Slide 4: Some material comparisons
Properties are for 100% TD | Li2O | Li4SiO4 | Li2TiO3 | Li2ZrO3
Lithium density (g/cm3) | 0.94 | 0.51 | 0.43 | 0.38
Min-max Temp for tritium release (°C) | 397-795 | 325-925 | <900 | 400-1400
Reactivity w/ H2O | High | Little | Less | Less
Crush Load (N) | - | Low | High | High
Residence time @400°C (h) | 10 | 2 | 2 | 1

## Slide 5: Example pebble production
Mixing
Shaping
Sintering
Li2TiO3 Powder
PVA Solution
Mixing
Dropping into Glycerin
including Boric Acid
Drying
Sintering
Fabrication Process
PVA Solution
Li2TiO3 Powder

## Slide 6: Effect of Sintering Time (1200oC, air atmosphere)
Sintering Time : 1 h
Sintering Time : 2 h
Sintering Time : 3 h
Sintering Time : 4 h
1mm
1mm
1mm
1mm
Avg. Dia. : 1.00 mm
Avg. Dia. : 1.03 mm
Avg. Dia. : 1.01 mm
Avg. Dia. : 0.98 mm
50μm
50μm
50μm
open porosity ~ 10%

## Slide 7: Sphere-sphere contact mechanics
P(r)
r
a
z

## Slide 8: Transient Discrete Element Method
J
I
Q

## Slide 9
Filling  packing  heating
Contact force probability distribution
Simulating oedometric compression

## Slide 11
Chart: Maximum Temperatures
| Li2O | LiAlO2 | Li2SiO3 | Li2Si | LiAl | Li7Pb2 | Li2TiO3 | Li2ZrO3 | Li4SiO4
STARFIRE, 1981 | 910 | 850 | 610 | 420 | 380 | 390
Clemmer, 1980 | 910 | 850 | 610 | 350 | 310 | 330 | 820 | 860
Johnson et al., 1988 | 800 | 832 | 800 | 981 | 666
Johnson & Clemmer, 1981 | 750 | 855 | 820 | 860 | 670

## Slide 12: Single pebble properties
Vacuum chamber
Inconel pistons
Graphite heater
Pebble location
Chart: Displacement (mm)

## Slide 13: Pebble failure prediction: strain energy
Lab tests
Ensemble

## Slide 14: Pebble bed designs (Japanese solid breeder)
Surface Heat Flux: 1MW/m2
Neutron Wall Load: 5MW/m2 (1.5×1015n/cm2s)
Coolant flow
Purge gas

## Slide 15: Engineering data of pebble bed thermomechanics
Pebble bed thermo-physical and mechanical data
Effective thermal conductivity
Effective modulus
Thermal creep correlation
Effective thermal expansion rate
Pebble bed failure data
Increase of effective thermal conductivity with compressive and creep strain
Bed–wall interface thermomechanical data
Heat conductance
Friction coefficient

## Slide 16: Effective thermal conductivity - ceramic
Li4SiO4
Li2TiO3
Thermocouples
Pulse of current

## Slide 17: Creep properties of ceramic pebble beds
0.19
0.65
6947
0.37
JAERI-Li2TiO3
0.18
0.65
7576
0.67
CEA-Li2TiO3
0.2
0.65
10220
12.12
FZK-Li4SiO4
n
p
B
A
ecr(t) = A exp(-B/T(K)) s(MPa)p t(s)n
Granular
material
m
e
t
a
t
i
t
a
n
a
t
e
p
e
b
b
l
e
b
e
d
s
T
=
7
5
0
°
C
T
s
d
g
s
(
°
C
)
(
%
)
(
m
m
)
T
i
-
B
:
9
5
0
8
7
0
.
5
-
1
T
i
-
D
:
1
0
4
0
9
2
1
-
2
T
i
-
D
l
t
a
:
"
"
2
5
T
i
-
A
:
1
0
5
0
9
5
1
.
5
-
2
.
5
T
i
-
E
:
1
1
0
0
8
6
1
-
5
T
i
-
G
:
1
1
0
0
8
9
1
-
5
T
i
-
H
:
1
1
0
0
9
1
1
-
3
T
i
-
F
:
1
1
4
0
9
0
2
-
7
T
i
-
I
:
1
2
0
0
9
2
1
0
-
5
0
T
i
-
J
:
1
2
0
0
8
4
1
-
3
T
i
-
K
:
1
2
0
0
8
3
1
-
3
100
1000
10000
Creep Time [min]
1
Creep Strain [%]
2
3

## Slide 18: Effective thermal expansion
Li2TiO3
10x higher than bulk material

## Slide 19: Effective properties - Beryllium
Be Pebbles after compression
Application of Hot Wire Method
HECOP
Steady-state method

## Slide 20: Demonstrating effective conductivity, modulus, plastic rearrangement
Beryllium
(k = 200 W/mK)

## Slide 21: Continuum material treatment of pebble bed

## Slide 22: UCLA’s “unified cap” implementation of FEM
W, D1, D2, and X0 are empirically derived constants
A1-3, s, E0 are empirically derived T-dependent constants
C1, C2, C3, and C4 are empirically derived constants
Example curves
Features:
1) A unified yielding surface for both cap and shear portions;
2) Strain-dependent creep law better reflecting the localized creep behavior of pebble bed.
R, K0, σ0, and α are empirically derived constants

## Slide 23
Stress/strain during loading and unloading
Temperature distribution (oC)
Plastic strain distribution along the Y-direction
Stress distribution along the Y-direction (Pa)

## Slide 24: FEM coupling with DEM
Finite element treatment of pebble beds can give advanced understanding of interaction at the outset
Gap formation from settling and pebble damage still a major issue
Can FEM simulations integrate with DEM to intermittently provide new packing formations?
g
Containing structure
FEM-derived pebble bed volume after compaction
Gap poorly handled in FEM
DEM predicts the pebbles to settle and fill the gap

## Slide 25: Closing remarks for thermomechanics
Good…
Non-mobile breeder avoids many of the problems associated with liquid breeders
  Pressure drop
  Corrosion
  Large external inventory of lithium
Not so good…
Low thermal conductivity of ceramic
  Decreased further in pebble form
  Decreased yet again under irradiation
Bound by a temperature window
  for bulk diffusion of tritium in ceramic
  to avoid sintering
Low k and temperature window combine to limit power density and potentially achievable TBR

## Slide 26: Advanced material investigations
Grains on the outside of a pebble before sintering
Grains on a pebble after spark plasma sintering
Ceramic foam
Sharafat, S., Ghoniem, N., Sawan, M. E., Ying, A., & Williams, B. (2006)
Spark-plasma Sintering